### SELECTION 78                                                        5/23/06

Selection 78 series is a range of lead-and cadmium-free (*1), intermixable, resistant inglaze colors for porcelain.

(*1) 78311 yellow, 78312 yellow, 78316 orange, 78619 red and 78630 red are contain cadmium as inclusion pigment.

#### FIRING CONDITIONS

| Porcelain | 1,180 - 1,250℃ |
| --- | --- |
| Stoneware | 1,160 - 1,200℃ |
| Bone China | 1,000 - 1,050℃ |
| Vitreous China | 1,000 - 1,100℃ |

Selection 78 colors are suitable for fast-firing conditions, 60-150 minutes cold to cold.

Gold-containing colors, 78902 pink, 78907 magenta and 78918 maroon are recommended for firing bellow 1,230 ℃.

#### APPLICATION

Selection 78 colors are suitable for screen-transfer printing, direct printing, spraying, pad printing and hand painting.

#### MESH SIZE

Recommend mesh sizes are 180-300 mesh (71-120T) for all screen applications.

#### MEDIUM RATIO

| Color : Medium | 10 : 7 - 8 |
| --- | --- |
| Flux : Medium | 10 : 10 - 12 |

We recommend PM2 normal-printing medium and PMT9 thixsotropic medium.

We recommend C33 cover coat by printing 70 mesh (27T).

Lead-free colors absorb any moisture easily, therefore keep powder colors in a dry place. We recommend drying the color powder before using.

#### MISCIBILITY

Selection 78 colors can be mixed with each other in any proportions. However, we recommended that 78806 cobalt blue should not be mixed with gold containing colors, 78902 pink, 78907 magenta and 78918 maroon. To obtain pastel color tone, it is suitable to use 78201 mixing white or 78202 white. 78101 flux is suitable for mixing and overprinting. Overprinting 78101 flux can improve color gloss and stability in high firing temperature. 78806 cobalt blue is not recommended 78101 overprinting.

#### FOUR-COLOR PRINTING

#### Choice of four colors

| Yellow | 78312 yellow |
| --- | --- |
| Magenta | 78907 magenta, 78918 maroon |
| Cyan | 78804 cyan |
| Black | 78706 black |
| Flux | 78101 flux |

78312 yellow can be mixed with 78321 yellow, 78311 yellow or 78316 orange to adjust yellow tone.

78907 magenta and 78918 maroon can be mixed each other. They can be mixed with 78619 red and 78630 red.

78619 red and 78630 red can be overprinted on these for-colors.

###### Printing order

- yellow → magenta → red (if necessary) → cyan→ black→ flux

###### Mesh size

Recommend mesh sizes are 300-330 mesh (120-130T).

Medium ratio

We recommend printing by PMT9 thixsotropic medium and C33 cover coat.

| Yellow : PMT9 | 10 : 6.5 - 7 |
| --- | --- |
| Magenta : PMT9 | 10 : 7.5 –8.0 |
| Cyan : PMT9 | 10 : 7.0 –7.5 |
| Black : PMT9 | 10 : 7.0 –7.5 |
| Flux : PMT9 | 10 : 10 - 12 |

CHEMICAL DURABILITY

Residual lead and cadmium content

SELECTION 78 colors are well controlled and do not need additional lead and cadmium, with some exceptions (*1 cadmium-containing colors). The contamination of residual lead is less than 600 ppm (0.06wt%) and of cadmium is less than 100 ppm (0.01wt%). They are, therefore, in compliance with Californian Proposition 65 requirements.

Lead and cadmium release

According to DI EN 1388-1-2 test, SELECTION 78 colors do not show lead and cadmium releases and they are bellow AAS limits.

Acid resistance

SELECTION 78 colors show no visible attack after immersion in a 3% hydrochloric acid solution for 6 hours at 20℃.

Alkali resistance

SELECTION 78 colors show no visible attack after immersion in a 0.5% calgonite solution for 24 hours at 77 ℃. They are also high dishwasher resistant.

SAFETY DATA SHEET (MSDS)

Safety data sheet of all of Selection 78 colors are available.

The above information and statements are unsolicited. Izawa Pigment Co., Ltd. provides them to promote its products. The above information and statements are also believed to be accurate at the time of publication under their laboratory conditions. Use of them is at the sole discretion of the user and Izawa Pigment Co. Ltd. does not give any warranty with respect to any test results. In no event shall Izawa Pigment Co., Ltd. be liable for any direct, indirect, special, incidental, or consequential damages arising out of the use of the above information.